QUALITY CONTROL LABORATORY CERTIFICATE OF ANALYSIS SOLID PARAFFIN WAX OF 1.5-2.5% OIL CONTENT SRL NO CHARACTERISTICS METHOD RESULT 1 MELTING POINT ASTM D 127-63 58-60 2 OIL CONTENT ASTM D 721-68 1.5-2.5% 3 ASH CONTENT ASTM D 482-74 0.003% 4 ACIDITY ASTM D 974-64 0 5 ORGANIC -------------------- 0.0031 6 INORGANIC -------------------- 0 7 SMELL -------------------- ODOURLESS 8 COLOUR -------------------- WHITE